NOTIFICATION

The following notification is being circulated in accordance with Article 10.6

| 1. | Notifying Member: Rwanda If applicable, name of local government involved (Article 3.2 and 7.2): |
| --- | --- |
| 2. | Agency responsible: Rwanda Standards Board (RSB) Name and address (including telephone and fax numbers, email and website addresses, if available) of agency or authority designated to handle comments regarding the notification shall be indicated if different from above: Rwanda Standards Board KK 15 Rd, 49 P.O.BOX 7099, Kigali, Rwanda Tel: +250 788303492 Email: info@rsb.gov.rw Website: www.rsb.gov.rw |
| 3. | Notified under Article 2.9.2 [X], 2.10.1 [ ], 5.6.2 [ ], 5.7.1 [ ], other: |
| 4. | Products covered (HS or CCCN where applicable, otherwise national tariff heading. ICS numbers may be provided in addition, where applicable): Paints and varnishes (ICS 87.040) |
| 5. | Title, number of pages and language(s) of the notified document: DRS 466: 2021, Two-Pack Epoxy enamel, glossy paint — Specification (21 page(s), in English) |
| 6. | Description of content: This Rwanda Draft Standard prescribes requirements, sampling and test methods for two components epoxy enamel used as a finish coat for the painting of steel plant equipment where protection to salt water, chemicals, mineral oils, solvents and resistance to moisture protection in marine environment. |
| 7. | Objective and rationale, including the nature of urgent problems where applicable: Consumer information, labelling; Prevention of deceptive practices and consumer protection; Quality requirements; Reducing trade barriers and facilitating trade |
| 8. | Relevant documents: ISO 4618, Paints and varnishes — Terms and definitions ISO 1523, Determination of flash point — Closed cup equilibrium method ISO 9117-1, Paints and varnishes — Drying tests — Part 1: Determination of through-dry state and through-dry time ISO 9117-3, Paints and varnishes — Drying tests — Part 3: Surface-drying test using ballotoni ISO 3251, Paints, varnishes and plastics — Determination of non-volatile-matter content ISO 6503, Paints and varnishes — Determination of total lead — Flame atomic absorption spectrometric method ISO 3856-6, Paints and varnishes — Determination of "soluble" metal — Part 6: Determination of total chromium content of the liquid portion of the paint — Flame atomic absorption spectrometric method ISO 9514, Paints and varnishes — Determination of the pot life of multicomponent coating systems — Preparation and condition of samples and guidelines for testing. ISO 2808, Paints and varnishes — Determination of film thickness ISO 2813, Paints and varnishes — Determination of gloss value at 20°, 60° and 85° ASTM F735-17, Standard test method for abrasion resistance of transparent plastics and coatings using the oscillating sand method RS OIML R 87, Quantity of product in pre-packages ISO 15528, Paints, varnishes and raw materials for paints and varnishes — Sampling |
| 9. | Proposed date of adoption: To be determined Proposed date of entry into force: to be determined |
| 10. | Final date for comments: 60 days from notification |
| 11. | Texts available from: National enquiry point [X] or address, telephone and fax numbers and email and website addresses, if available, of other body: KK 15 Rd, 49 Toll Free: 3250 Tel: +250 788303492 Email: info@rsb.gov.rw Website: www.rsb.gov.rw P.O.BOX 7099, Kigali, Rwanda https://members.wto.org/crnattachments/2021/TBT/RWA/21_4879_00_e.pdf |