NOTIFICATION

The following notification is being circulated in accordance with Article 10.6

| 1. | Notifying Member: THAILAND If applicable, name of local government involved (Article 3.2 and 7.2): |
| --- | --- |
| 2. | Agency responsible: Thai Industrial Standards Institute (TISI), Ministry of Industry Name and address (including telephone and fax numbers, email and website addresses, if available) of agency or authority designated to handle comments regarding the notification shall be indicated if different from above: WTO/TBT Enquiry Point and Notification Authority Thai Industrial Standards Institute (TISI), Ministry of Industry Tel: (662) 430 6831 ext. 2130 Fax: (662) 354 3041 E-mail: thaitbt@tisi.mail.go.th Website: https://www.tisi.go.th |
| 3. | Notified under Article 2.9.2 [X], 2.10.1 [ ], 5.6.2 [ ], 5.7.1 [ ],3.2 [ ], 7.2 [ ], other : |
| 4. | Products covered (HS or CCCN where applicable, otherwise national tariff heading. ICS numbers may be provided in addition, where applicable): Hot-Dip Zinc-Coated Cold Reduced Flat Steel (ICS 77.140.50) |
| 5. | Title, number of pages and language(s) of the notified document: Draft Ministerial Regulation on Hot-Dip Zinc-Coated Cold Reduced Flat Steel (TIS 50-25xx (20xx) ; (36 page(s), in Thai) |
| 6. | Description of content: The draft ministerial regulation mandates hot-dip zinc-coated cold reduced flat steel to comply with the standard TIS 50-25xx (20xx) TIS 50-25xx (20xx) covers: - Hot-dip zinc-coated cold reduces flat steel coated by substance mainly composed of zinc to improve rust protection properties and may be processed by chemical treatment, oil coating for more varied applications, in form of sheets, strips and corrugated sheets. - Hot-dip zinc-coated cold reduced flat steel with a nominal thickness up to 3.20 mm. - Hot-dip zinc-coated cold reduced flat steel corrugated sheet with a minimum thickness of 0.11 mm, with pitch of 76 mm and depth of 18 mm (large corrugated), and pitch of 32 mm and depth of 9 mm (small corrugated). TIS 50-25xx (20xx) excludes: - Hot-dip zinc-coated cold reduced flat steel contained with zinc-ferrous alloy layer (galvanneal) - Hot-dip zinc-coated cold reduced flat steel for automobile uses, which are already developed as industrial products standards. - Hot-dip zinc-coated cold reduced flat steel alloy with other metals, which are already developed as industrial products standards, such as hot-dip zinc-5% to 13% aluminium-2% to 4% magnesium alloy-coated flat steel TIS 50-25xx (20xx) specifies scope, definitions, types, grades and surface finishes, dimensions and normative tolerances, chemical compositions, requirements, marking and labelling, sampling and criteria for conformity, and testing. |
| 7. | Objective and rationale, including the nature of urgent problems where applicable: Protection of human health or safety |
| 8. | Relevant documents: ASTM A902–18a Standard Terminology Relating to Metallic Coated Steel Products JIS G 3302: 2019 Hot-dip zinc-coated steel sheet and strip JIS G 3316: 1987 Shapes and dimensions of corrugated steel sheets JIS G 0320: 2009 Standard test method for heat analysis of steel products JIS G 0320: 2009/ Standard test method for heat analysis of steel products (Amendment 1) AMENDMENT 1: 2015 JIS G 0320: 2009/ Standard test method for heat analysis of steel products (Amendment 2) AMENDMENT 2: 2017 JIS G 0321:2017 Product analysis and its tolerance for wrought steel JIS G 0404: 2014 Steel and steel products – General technical delivery requirements JIS G 3193: 2019 Dimensions, shape, mass and permissible variations of hot rolled steel plates, sheets and strips JIS K 0119: 2008 General rules for X-ray fluorescence analysis JIS Z 2241: 2020 Metallic materials - Tensile testing - Method of test at room temperature JIS Z 2244: 2018 Vickers hardness test - Test method JIS Z 2245: 2021 Rockwell hardness test - Test method JIS Z 8401: 2019 Rounding of numbers |
| 9. | Proposed date of adoption: To be determined Proposed date of entry into force: To be determined |
| 10. | Final date for comments: 60 days from notification |
| 11. | Texts available from: National enquiry point [ ] or address, telephone and fax numbers and email and website addresses, if available, of other body: WTO/TBT Enquiry Point and Notification Authority Thai Industrial Standards Institute (TISI), Ministry of Industry Tel: (662) 430 6831 ext. 2130 Fax: (662) 202 3511, 354 3041 E-mail: thaitbt@tisi.mail.go.th Website: https://www.tisi.go.th https://members.wto.org/crnattachments/2022/TBT/THA/22_2462_00_x.pdf |